Ultrashort laser pulse induction of diverse morphology nanostructures on thin films

Kernius Vilkevičius1,*, George D. Tsibidis2, Algirdas Seskis3, Emmanuel Stratakis2,4, and Evaldas Stankevičius1

1 Department of Laser Technologies, Center for Physical Sciences and Technology, Savanoriu Ave. 231, 02300, Vilnius, Lithuania

2 Institute of Electronic Structure and Laser (IESL), Foundation for Research and Technology (FORTH), Vassilika Vouton, 70013, Heraklion, Crete, Greece

3 Department of Characterization of Materials, Center for Physical Sciences and Technology, Sauletekio Ave. 3, 10257, Vilnius, Lithuania

4 Department of Physics, University of Crete, 71003, Heraklion, Greece

*Corresponding author email: kernius.vilkevicius@ftmc.lt

Ultrashort laser pulses are applied to thin metal films to induce the formation of diverse morphology nanostructures that depend on the pulse energy [1]. The shape of the structure plays a decisive role in determining the optical properties, so control of the morphology is pivotal. The formation of gold structures fabricated using single pulses is determined to be due to the thermoelastic stress and surface tension [2]. The periodic arrangement of metallic nanostructures enables the excitation of hybridized plasmonic modes, resulting in the narrowing and enhancement of plasmon resonance [3]. Since the structures are formed on the metal with plain film among them, the propagating surface polariton couples with surface lattice resonance, producing a dispersive and high-quality resonance.

The formation of single-pulse-induced structures on 25, 50, 75, and 100 nm gold thicknesses using direct laser writing was investigated. The required pulse fluence was determined for each thickness to obtain the corresponding morphology – bumps, cones, or jets. The created theoretical model described the induced thermal effects. Additionally, the manipulation in shape by changing the grating period was in detail investigated. Reducing the distance between the structures modifies the morphology, providing an additional degree of freedom to control the shape. Finally, the plasmonic properties of these gratings were investigated. The resonant wavelength and quality are highly dependent on the morphology, and increasing the size of the structure results in a shift towards longer wavelengths.

Acknowledgements: E.S. and K.V. has received funding from the Research Council of Lithuania (LMT, Lithuania) under the project No. S-MIP-23-32 and from the Nanoscience Foundries and Fine Analysis – Europe (NFFA-Europe) under the project ID 369.

References: [1] D. Pavlov, S. Syubaev, A. Kuchmizhak, S. Gurbatov, O. Vitrik, et al., Direct laser printing of tunable IR resonant nanoantenna arrays. Appl. Surf. Sci., 469, 514–520, (2019); [2] Y.P. Meshcheryakov, N.M. Bulgakova, Thermoelastic modeling of microbump and nanojet formation on nanosize gold films under femtosecond laser irradiation, Appl. Phys. A, 82(2), 363–368 (2006). [3] E. Stankevičius, K. Vilkevičius, M. Gedvilas, E. Bužavaitė‐Vertelienė, A. Selskis, et al., Direct Laser Writing for the Formation of Large‐Scale Gold Microbumps Arrays Generating Hybrid Lattice Plasmon Polaritons in Vis–NIR Range. Adv. Opt. Mater., 9(12), 2100027 (2021).