Bi-stability control in extremely efficient laser ablation by MHz burst of femtosecond pulses: experiment, modeling, and applications

Andrius Žemaitis, Mantas Gaidys, Saulė Steponavičiūtė, Paulius Gečys, Mindaugas Gedvilas*

Department of Laser Technologies (LTS), Center for Physical Sciences and Technology (FTMC), Savanorių Ave. 231, 02300 Vilnius, Lithuania

*Corresponding author email: mgedvilas@ftmc.lt

This study investigates the controllable bi-stable behavior observed in laser ablation efficiency and surface roughness, manipulated by adjusting burst fluence and burst length [1]. The presence of plasma shielding from the incoming laser radiation leads to a notable reduction in ablation efficiency specifically for an even number of pulses within the burst. A toy model dedicated to ablation efficiency calculation taking into account the attenuation of incoming laser radiation by plasma generated from preceding pulses, yielding a mathematical recurrence relation was introduced. This relation connects the ablation efficiency of consecutive pulses, thereby predicting bi-stability and sudden jumps in efficiency upon the number of pulses within the burst and variations in the burst laser fluence as control parameters. Modeling results employing this novel recurrence relation demonstrate both stable and bi-stable ablation efficiencies depending on burst fluence and burst length, having strong agreement with experimental observations. Notably, optimizing the shielding effect through the use of three pulses within the burst has led to exceptionally efficient laser ablation of 5.66 µm3/µJ [1], surpassing the highest value documented in scientific literature [2]. High-quality, intricate 3D cavities designed for LED micro-optics were laser-machined [1] by using a layer-by-layer milling technique [3] and then polished employing burst processing regimes [4] that had the lowest roughness and maximum ablation rate. The laser-induced periodical surface structure (LIPSS) formation has also been investigated. Wettability control by creating LIPSS or other types of micro/nanostructures at a high processing rate has been demonstrated.

Acknowledgements:

Central Project Management Agency (CPVA) 10-038-T-0009.

References:

[1] A. Žemaitis, M. Gaidys, P. Gečys, M. Gedvilas, Bi-stability in femtosecond laser ablation by MHz bursts, Sci. Rep. In Press (2024). DOI: 10.1038/s41598-024-54928-7.

[2] A. Žemaitis, M. Gaidys, P. Gečys, M. Barkauskas, M. Gedvilas,  Femtosecond laser ablation by bibursts in the MHz and GHz pulse repetition rates, Opt. Express 29, 7641 (2021). DOI: 10.1364/OE.417883.

[3] A. Žemaitis, P. Gečys, M. Gedvilas, High throughput and low surface roughness laser layer-by-layer milling using nanosecond (ns), picosecond (ps), and hybrid ns-ps pulses: A comparative study, Opt. Lasers Eng. 176, 108046 (2024). DOI: 10.1016/j.optlaseng.2024.108046.

[4] M. Gaidys, A. Žemaitis, P. Gečys, M. Gedvilas, Efficient surface polishing using burst and biburst mode ultrafast laser irradiation, RSC Adv. 13, 3586 (2023). DOI: 10.1039/D2RA05208C.