Two Photon Polymerization for Inertial Fusion Energy Target Fabrication

Fabian Christ1,2*, Gabriel Schaumann1,2, Nils Schott1,2, Johanna Vetter3,
Andreas Blaeser3, and Markus Roth1,2

1 Institute of Nuclear Physics, Technical University of Darmstadt, Schlossgartenstraße 9, 64289 Darmstadt, Hesse, Germany

2 Focused Energy GmbH, Im Tiefen See 45, 64293, Darmstadt, Hesse, Germany

3 Institute of Printing Science and Technology, Technical University of Darmstadt, Magdalenenstraße 2, 64289 Darmstadt, Hesse, Germany

*Corresponding author email: fchrist@ikp.tu-darmstadt.de

Nuclear fusion as a clean, secure, and dependable energy source is receiving enormous global interest since it arises as a promising solution to the energy and climate crisis. Recently, scientific breakeven was demonstrated for laser-driven inertial confinement fusion, further motivating the development of this approach [1]. A crucial component for the success of laser-driven inertial fusion energy is the fuel capsule (target). A minimal feature size of a few micrometers and the need for a reliable repeatability are essential. That poses high requirements on its manufacturing process.

In this work, we use a direct drive, proton fast ignition target that consists of a spherical foam-shell with a metallic cone placed inside, as proposed in [2]. Here we focus on the fabrication of the foam-shell utilizing Two Photon Polymerization (2PP) as a nanoscale additive manufacturing technique. Despite its limiting fabrication time, 2PP excels at all other production requirements. The figure displays the successful fabrication of a foam-shell target with a diameter of 1.8 mm employing the Photonic Professional GT2 from Nanoscribe. Foam properties are optimized to ensure a homogeneous distribution of the fusion fuel while mitigating negative effects on the implosion dynamics.

This study examines the impact of the foam structure and various printing parameters on the fabrication time, target quality, and stability. Several foam structures were printed under varying conditions. Furthermore, this work outlines three problems and limitations: stitching errors, data handling, and long fabrication times. First, stitching errors can occur when printing large objects that exceed the printing field of the objective and are separated into individual blocks printed in succession. Second, the large discrepancy between target dimension and minimal feature size generates tremendous amounts of data, limiting the minimum resolution. Third, the long printing time due to the point-to-point interaction is a major limitation that prevents 2PP from becoming a scalable target fabrication technique for a fusion power plant. We examine the influential factors, explore possibilities for future optimization and define general limitations.

Acknowledgements:

The target structures were printed on a Nanoscribe printer funded by the DFG program 496890651: “Microfabrication system based on two-photon lithography” and the Loewe project Flow for Life.

# References

| [1] | E. Cartlidge, "National Ignition Facility demonstrates net fusion energy gain," Physics World, 2023. |
| --- | --- |
| [2] | M. Roth et al., "Fast Ignition by Intense Laser-Accelerated Proton Beams," Physical Review Letters, pp. 436-439, 2001. |