The use of femtosecond UV laser for selective layer processing of CIGS thin-film solar cells

Denys I. Miakota1,*, Asbjørn Meldgaard Moltke2, Callum Robertson Smith2,

Ole Bang2, Andreas Zimmerman3, and Stela Canulescu1,**

1,2Department of Electrical and Photonics Engineering, Technical University of Denmark,

1Frederiksborgvej, 399, DK-4000 Roskilde; 2Ørsted Plads 343, Kgs. Lyngby DK-2800, Denmark

3Sunplugged GmbH, Affenhausen 1, 6413 Wildermieming, Austria

*Corresponding author email: *denmi@dtu.dk; **stec@dtu.dk

Thin-film photovoltaics (PV) hold great potential for low-cost, high-performance, and flexible solar panel production, even though the PV market is dominated by crystalline silicon technologies. Cu(In,Ga)Se2 (CIGS) based thin-film solar cells are one of the most promising technologies, where recently conversion efficiencies reaching up to 23.6% have been demonstrated on rigid glass substrates [1]. The high efficiency of CIGS thin-film solar cells can be maintained in a full PV panel by subdividing area into small segments that are interconnected in series. This way the photocurrent is limited, reducing resistive losses in thin layers. The series connections consist of three scribing processes called P1, P2, and P3 where the number stands for the coating process step after which they are applied [2] (Figure 1 shows cross-section of a typical CIGS stack and scribing processes P1, P2, P3 type I, and P3 type II).

Here, we will present our findings on high-precision CIGS solar cell processing P1, P2, and P3 using femtosecond (<100 fs) supercontinuum pulsed laser with a tunable UV wavelength. Femtosecond pulses enable highly localized heating due to a time scale shorter than the electron–phonon equilibrium time. This may offer a low heat-affected zone and prevent undesirable melting of CIGS, which causes phase transition and creates conductive channels [3], which cause shortcuts and reduce overall PV module performance. By using femtosecond laser operating at UV wavelength above the bandgap of Al:ZnO we can enable highly controlled P3 scribing due to strong absorption in all the layers. The dependence of ablation depth on laser fluence and overlap ratio will be experimentally studied, with discussions on the corresponding ablation mechanisms.

Figure 1. CIGS solar cell scribing types. a) CIGS solar cell layer structure; b) P1 isolative Mo back-contact patterning; c) P2 CIGS layer removal; d) delicate insulating P3 type-I scribing with top Al:ZnO removal; e) P3 type-II cell insulating scribe with layers removal down to Mo back-contact.

Acknowledgements: The authors acknowledge financial support from Innovation Fund Denmark (project UVSOLAR, No. 2081-00016A) and from Villum Fonden (2021 Villum Investigator project No. 00037822: Table-Top Synchrotrons).

References: [1] Keller, J., Kiselman, K., et. al. Nat. Energy (2024); [2] Andreas Burn et. al., Proc. SPIE 8243, Laser Applications in Microelectronic and Optoelectronic Manufacturing XVII, 824318 (2012); [3] Hermann, J. et.al., J. Phys. D: Appl. Phys. 39 453 (2006)